Best catalyst for different ArCH2OH

Data stracture in all cells: (TONmax/T,°C/base/catalyst/atmosphere/doi/year/comment)

| Metal | Number of papers | Maximal TON among all | Maximal TON among the processes with preparative yields >65% | The lowest temperature among all with preparative yields >65% | The highest TON in the absence of base | The lowest temperature in the absence of base with preparative yields >65% | most popular working bases |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ru | 8 | (364/150.0°C/no base/Ru(CO)H2(PPh3)3/inert/10.1021/ol1020527/2010) | (364/150.0°C/no base/Ru(CO)H2(PPh3)3/inert/10.1021/ol1020527/2010) | (33/120.0°C/KOt-Amyl/(p-cymene)Ru(NHC1^NHC1)ClPF6/inert/10.1002/chem.201603901/2016) | (364/150.0°C/no base/Ru(CO)H2(PPh3)3/inert/10.1021/ol1020527/2010) | (352/150.0°C/no base/Ru(CO)H2(PPh3)3/inert/10.1021/ol1020527/2010) | ['K2CO3', 'no base', 'KHCO3'] |
| Au | 3 | (1517/150.0°C/K2CO3/Au/Ag-Mo-NR/inert/10.1039/c2cc34178f/2012) | (1517/150.0°C/K2CO3/Au/Ag-Mo-NR/inert/10.1039/c2cc34178f/2012) | (192/120.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201100393/2011) | (198/120.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201100393/2011) | (192/120.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201100393/2011) | ['no base', 'K2CO3'] |
| Ir | 3 | (492/130.0°C/K2CO3/Cp*Ir(N^N)Cl2/inert/10.1021/acs.joc.1c02625/2021) | (492/130.0°C/K2CO3/Cp*Ir(N^N)Cl2/inert/10.1021/acs.joc.1c02625/2021) | (81/100.0°C/tBuOK/Cp*IrCl(N^O)1/inert/10.1021/acs.inorgchem.2c00703/2022) | no data | no data | ['K2CO3', 'tBuOK', 'Cs2CO3'] |
| Pd | 3 | (960/25.0°C/K3PO4/Pd/NH2-MIL-101(Fe)-2MI(300)/inert/10.1016/j.jcat.2020.05.033/2020) | (960/25.0°C/K3PO4/Pd/NH2-MIL-101(Fe)-2MI(300)/inert/10.1016/j.jcat.2020.05.033/2020) | (189/25.0°C/no base/Pd-Ti-NS/inert/10.1016/j.jcat.2018.02.005/2018) | (219/25.0°C/no base/Pd-Ti-NS/inert/10.1016/j.jcat.2018.02.005/2018) | (189/25.0°C/no base/Pd-Ti-NS/inert/10.1016/j.jcat.2018.02.005/2018) | ['tBuOK', 'K3PO4', 'no base'] |
| Co | 1 | (6/160.0°C/no base/Co-N-C/CNT@AC/inert/10.1039/c8gc03818j/2019) | (6/160.0°C/no base/Co-N-C/CNT@AC/inert/10.1039/c8gc03818j/2019) | (6/160.0°C/no base/Co-N-C/CNT@AC/inert/10.1039/c8gc03818j/2019) | (6/160.0°C/no base/Co-N-C/CNT@AC/inert/10.1039/c8gc03818j/2019) | (6/160.0°C/no base/Co-N-C/CNT@AC/inert/10.1039/c8gc03818j/2019) | ['no base'] |
| Mo | 1 | (18/150.0°C/tBuOK/Mo(NHC3)2(CO)4/inert/10.1021/acscatal.1c02956/2021) | (18/150.0°C/tBuOK/Mo(NHC3)2(CO)4/inert/10.1021/acscatal.1c02956/2021) | (16/150.0°C/tBuOK/Mo(NHC3)2(CO)4/inert/10.1021/acscatal.1c02956/2021) | no data | no data | ['tBuOK'] |
| Ag | 1 | (45/140.0°C/Cs2CO3/Ag/Al2O3/inert/10.1039/c5cp00330j/2015) | (45/140.0°C/Cs2CO3/Ag/Al2O3/inert/10.1039/c5cp00330j/2015) | (40/140.0°C/Cs2CO3/Ag/Al2O3/inert/10.1039/c5cp00330j/2015) | no data | no data | ['Cs2CO3'] |