Best catalysts by metals for PhNH2 + BnOH process

Data stracture in all cells: (TONmax/T,°C/base/catalyst/atmosphere/doi/year/comment)

| Metal | Number of papers | Maximal TON among all | Maximal TON among the processes with preparative yields >65% | The lowest temperature among all with preparative yields >65% | The highest TON in the absence of base | The lowest temperature in the absence of base with preparative yields >65% | most popular working bases |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ru | 66 | (42840/110.0°C/tBuOK/Ru(1,10-phenanthroline)Py(PPh3)2(PF6)/inert/10.1002/adsc.201701117/2017/0) | (12833/170.0°C/no base/Ru@Beta/inert/https://doi.org/10.1016/j.cej.2024.152457/2024/0) | (76/25.0°C/tBuOK/[Ru(COD)Cl2]n/inert/10.1016/j.catcom.2017.03.007/2017/0) | (12833/170.0°C/no base/Ru@Beta/inert/https://doi.org/10.1016/j.cej.2024.152457/2024/0) | (83/70.0°C/no base/(p-cymene)Ru(L1)Cl/oxygen/10.1021/acs.orglett.1c02968/2021/0) | ['tBuOK', 'KOH'] |
| Ir | 59 | (1840/70.0°C/tBuOK/(Ir(cod)Ome)2/inert/10.1002/chem.201402952/2014/0) | (920/70.0°C/tBuOK/Ir*PNP complex/inert/10.1002/chem.201001871/2010/0) | (192/25.0°C/tBuOK/IrNHC/inert/10.1039/c3cc42669f/2013/0) | (890/78.0°C/no base/(2EtNHC)IrCp*Cl2/inert/10.1002/ejoc.202301105/2024/0) | (50/25.0°C/no base/(2EtNHC)IrCp*Cl2/inert/10.1002/ejoc.202301105/2024/0) | ['tBuOK', 'no base'] |
| Pd | 27 | (44500/130.0°C/LiOH/Pd2((AcO)pirazoleAr3)2/inert/10.1016/j.tet.2017.03.001/2017/0) | (44500/130.0°C/LiOH/Pd2((AcO)pirazoleAr3)2/inert/10.1016/j.tet.2017.03.001/2017/0) | (31/25.0°C/no base/Pd0,3/TiO2/inert/10.1021/cs300756f/2013/irradiation) | (553/160.0°C/no base/Pd/Fe2O3/inert/10.1016/j.tetlet.2011.01.059/2011/0) | (31/25.0°C/no base/Pd0,3/TiO2/inert/10.1021/cs300756f/2013/irradiation) | ['LiOH', 'no base'] |
| Co | 20 | (3256/140.0°C/tBuOK/Co1-N3P1/inert/10.1021/jacs.4c07197/2024/0) | (3256/140.0°C/tBuOK/Co1-N3P1/inert/10.1021/jacs.4c07197/2024/0) | (84/80.0°C/tBuOK/Co-PNP-pincer/inert/10.1021/acs.orglett.6b01647/2016/0) | (167/25.0°C/no base/Co/TiO2/inert/10.1016/j.apcatb.2022.121264/2022/14W blue LED) | (33/100.0°C/no base/Co-PNP-pincer/inert/10.1021/acs.orglett.5b03461/2015/0) | ['tBuOK', 'KOH'] |
| Cu | 19 | (367/100.0°C/KOH/Cu/Magnetitt/oxygen/10.1039/c3gc40818c/2013/0) | (367/100.0°C/KOH/Cu/Magnetitt/oxygen/10.1039/c3gc40818c/2013/0) | (70/25.0°C/no base/[CuNNO(OAc)]2/oxygen/10.1039/d2dt01771g/2022/12 W White LEDs) | (176/160.0°C/no base/Cu/CeO2-P/inert/10.1016/j.jcat.2023.01.020/2023/0) | (70/25.0°C/no base/[CuNNO(OAc)]2/oxygen/10.1039/d2dt01771g/2022/12 W White LEDs) | ['KOH', 'no base'] |
| Fe | 19 | (313/135.0°C/KOH/Fe20-SA@NSC/inert/10.1039/d1ta07673f/2021/0) | (313/135.0°C/KOH/Fe20-SA@NSC/inert/10.1039/d1ta07673f/2021/0) | (50/25.0°C/no base/Fe/TiO2/inert/10.1016/j.apcatb.2022.121264/2022/14W blue LED) | (50/25.0°C/no base/Fe/TiO2/inert/10.1016/j.apcatb.2022.121264/2022/14W blue LED) | (50/25.0°C/no base/Fe/TiO2/inert/10.1016/j.apcatb.2022.121264/2022/14W blue LED) | ['tBuOK', 'no base'] |
| Ni | 18 | (17500/200.0°C/tBuONa/NiNNN/inert/10.1021/acs.organomet.0c00233/2020/0) | (1720/130.0°C/tBuOK/NiN4Br/inert/10.1039/d2gc02206k/2022/0) | (26/100.0°C/no base/Ni/Ru@SBA/inert/10.1021/acssuschemeng.2c01092/2022/0) | (99/144.0°C/no base/Ni/θ-Al2O3/inert/10.1021/cs4001267/2013/0) | (26/100.0°C/no base/Ni/Ru@SBA/inert/10.1021/acssuschemeng.2c01092/2022/0) | ['tBuOK', 'KOH'] |
| Mn | 12 | (550/50.0°C/KH/Mn(CO)5Br/inert/10.1021/acs.orglett.9b00832/2019/0) | (277/50.0°C/KH/Mn(CO)5Br/inert/10.1021/acs.orglett.9b00832/2019/0) | (61/25.0°C/tBuOK/Mn(CO)3(NHC)2/inert/10.1039/c9cc02989c/2019/0) | (10/100.0°C/no base/Mn(NHC1)2(CO)3Br/inert/10.1021/acs.organomet.3c00046/2023/0) | no data | ['tBuOK', 'KH'] |
| Au | 10 | (11566/180.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201001848/2010/0) | (11566/180.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201001848/2010/0) | (8/100.0°C/tBuOK/Ph3PAuCl/inert/10.1016/j.tet.2014.10.007/2014/0) | (11566/180.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201001848/2010/0) | (20/110.0°C/no base/Au/ZrO2/inert/10.1016/j.apcata.2011.11.017/2011/0) | ['no base', 'tBuOK'] |
| Ag | 9 | (98/110.0°C/NaOH/Ag@MnO2/oxygen/10.1177/1747519821989963/2021/0) | (98/110.0°C/NaOH/Ag@MnO2/oxygen/10.1177/1747519821989963/2021/0) | (92/100.0°C/KOH/Fe3O4@SiO2-Ag (SMNP-Ag)/oxygen/10.1002/aoc.3720/2017/0) | (25/25.0°C/no base/Ag/TiO2/inert/10.1016/j.apcatb.2022.121264/2022/14W blue LED) | (24/145.0°C/no base/Ag/Al2O3-5/inert/10.1002/cctc.200900209/2009/0) | ['tBuOK', 'KOH'] |
| Rh | 9 | (980/100.0°C/tBuOK/Rh(I)(COD)(NHC)triazoleC6H5/CB/oxygen/10.1021/acs.inorgchem.7b02586/2017/0) | (196/100.0°C/no base/Cp*-S-Rh-N-anthracene-Cl/inert/10.1021/acs.organomet.8b00908/2019/0) | (196/100.0°C/no base/Cp*-S-Rh-N-anthracene-Cl/inert/10.1021/acs.organomet.8b00908/2019/0) | (196/100.0°C/no base/Cp*-S-Rh-N-anthracene-Cl/inert/10.1021/acs.organomet.8b00908/2019/0) | (196/100.0°C/no base/Cp*-S-Rh-N-anthracene-Cl/inert/10.1021/acs.organomet.8b00908/2019/0) | ['no base', 'tBuOK'] |
| Pt | 8 | (18627/160.0°C/no base/Pt-Sn/g-Al2O3 (0,05 mol% Pt)/inert/10.1016/j.tet.2016.11.029/2016/0) | (18627/160.0°C/no base/Pt-Sn/g-Al2O3 (0,05 mol% Pt)/inert/10.1016/j.tet.2016.11.029/2016/0) | (268/110.0°C/no base/PtSn/Al2O3 1:3/inert/10.1002/chem.201101725/2011/0) | (18627/160.0°C/no base/Pt-Sn/g-Al2O3 (0,05 mol% Pt)/inert/10.1016/j.tet.2016.11.029/2016/0) | (268/110.0°C/no base/PtSn/Al2O3 1:3/inert/10.1002/chem.201101725/2011/0) | ['no base', 'tBuOK'] |
| Ti | 5 | (19/160.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020/microwave) | (19/160.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020/microwave) | (2/120.0°C/KOH/TiO2 NP/inert/10.1002/slct.202300770/2023/0) | (19/160.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020/microwave) | (16/160.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000229/2020/microwave) | ['KOH', 'no base'] |
| Zn | 4 | (102/120.0°C/tBuOK/CNS@Zn1-AA/inert/10.3390/nano13030445/2023/0) | (102/120.0°C/tBuOK/CNS@Zn1-AA/inert/10.3390/nano13030445/2023/0) | (26/120.0°C/tBuOK/(NNN2)ZnCl2/inert/10.1021/acs.joc.2c01773/2022/0) | (9/120.0°C/no base/CNS@Zn1-AA/inert/10.3390/nano13030445/2023/0) | no data | ['tBuOK', 'KOH'] |
| Cr | 3 | (49/150.0°C/tBuOK/CrNNN/inert/10.1002/anie.202001704/2020/0) | (38/150.0°C/tBuOK/CrNNN/inert/10.1002/anie.202001704/2020/0) | (14/150.0°C/tBuOK/CrNNN/inert/10.1002/anie.202001704/2020/0) | (10/160.0°C/no base/Cr(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | ['tBuOK'] |
| Mo | 3 | (76/130.0°C/tBuOK/Mo-NHC/inert/10.1021/acscatal.1c02956/2021/0) | (76/130.0°C/tBuOK/Mo-NHC/inert/10.1021/acscatal.1c02956/2021/0) | (34/120.0°C/tBuOK/Mo(CO)6/oxygen/10.1016/j.mcat.2021.111415/2021/0) | (0/130.0°C/no base/Mo-NHC/inert/10.1021/acscatal.1c02956/2021/0) | no data | ['tBuOK', 'tBuONa'] |
| Al | 3 | (10/160.0°C/no base/AI(NTf2)5/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (10/160.0°C/no base/AI(NTf2)5/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| W | 2 | (142/130.0°C/tBuOK/W(CO)6/inert/10.1002/cssc.202002830/2020/0) | (142/130.0°C/tBuOK/W(CO)6/inert/10.1002/cssc.202002830/2020/0) | (74/130.0°C/tBuOK/W(CO)6/inert/10.1002/cssc.202002830/2020/0) | (14/140.0°C/no base/10WO3/ZrO2/oxygen/10.1039/d2ra00198e/2022/0) | no data | ['tBuOK'] |
| Cd | 2 | (0/160.0°C/no base/Cd(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (0/160.0°C/no base/Cd(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Bi | 2 | (1162/25.0°C/tBuOK/Bi-S3/s-Vs/inert/10.1039/d2ta06142b/2022/100W blue LED) | (1162/25.0°C/tBuOK/Bi-S3/s-Vs/inert/10.1039/d2ta06142b/2022/100W blue LED) | (1162/25.0°C/tBuOK/Bi-S3/s-Vs/inert/10.1039/d2ta06142b/2022/100W blue LED) | (10/160.0°C/no base/Bi(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | ['tBuOK'] |
| Sm | 2 | (30/140.0°C/tBuOK/SmI2/inert/10.1021/acs.joc.9b00717/2019/MW) | (30/140.0°C/tBuOK/SmI2/inert/10.1021/acs.joc.9b00717/2019/MW) | (30/140.0°C/tBuOK/SmI2/inert/10.1021/acs.joc.9b00717/2019/MW) | (12/160.0°C/no base/Sm(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | ['tBuOK'] |
| Re | 2 | (66/100.0°C/tBuOK/Re(NHC1)2(CO)3Br/inert/10.1021/acs.organomet.3c00046/2023/0) | (66/100.0°C/tBuOK/Re(NHC1)2(CO)3Br/inert/10.1021/acs.organomet.3c00046/2023/0) | (54/100.0°C/tBuOK/Re(NHC1)2(CO)3Cl/inert/10.1021/acs.organomet.3c00046/2023/0) | (8/150.0°C/no base/ReH7(Pcy3)2/inert/10.1016/j.tetlet.2014.05.068/2014/0) | (8/150.0°C/no base/ReH7(Pcy3)2/inert/10.1016/j.tetlet.2014.05.068/2014/0) | ['tBuOK', 'no base'] |
| Hf | 1 | (7/120.0°C/no base/Hf-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021/0) | (7/120.0°C/no base/Hf-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021/0) | (7/120.0°C/no base/Hf-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021/0) | (7/120.0°C/no base/Hf-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021/0) | (7/120.0°C/no base/Hf-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021/0) | ['no base'] |
| Yb | 1 | (18/160.0°C/no base/Yb(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | (18/160.0°C/no base/Yb(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | (18/160.0°C/no base/Yb(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | (18/160.0°C/no base/Yb(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | (18/160.0°C/no base/Yb(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | ['no base'] |
| Ba | 1 | (0/160.0°C/no base/Ba(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (0/160.0°C/no base/Ba(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Ga | 1 | (10/160.0°C/no base/Ga(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (10/160.0°C/no base/Ga(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Au,Pd | 1 | (74/180.0°C/no base/AuPd/MgO/inert/10.1002/chem.200901501/2009/0) | no data | no data | (74/180.0°C/no base/AuPd/MgO/inert/10.1002/chem.200901501/2009/0) | no data | [] |
| Li | 1 | (0/160.0°C/no base/Li(NTf2)/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (0/160.0°C/no base/Li(NTf2)/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Eu | 1 | (17/160.0°C/no base/Eu(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | (17/160.0°C/no base/Eu(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | (17/160.0°C/no base/Eu(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | (17/160.0°C/no base/Eu(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | (17/160.0°C/no base/Eu(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | ['no base'] |
| Y | 1 | (7/160.0°C/no base/Y(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (7/160.0°C/no base/Y(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Sb | 1 | (14/160.0°C/no base/Sb(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (14/160.0°C/no base/Sb(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (14/160.0°C/no base/Sb(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (14/160.0°C/no base/Sb(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (14/160.0°C/no base/Sb(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | ['no base'] |
| Pd,Pt | 1 | (100/180.0°C/no base/PdPt/MgO/inert/10.1002/chem.200901501/2009/0) | (100/180.0°C/no base/PdPt/MgO/inert/10.1002/chem.200901501/2009/0) | (100/180.0°C/no base/PdPt/MgO/inert/10.1002/chem.200901501/2009/0) | (100/180.0°C/no base/PdPt/MgO/inert/10.1002/chem.200901501/2009/0) | (100/180.0°C/no base/PdPt/MgO/inert/10.1002/chem.200901501/2009/0) | ['no base'] |
| Nd | 1 | (15/160.0°C/no base/Nd(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (15/160.0°C/no base/Nd(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (15/160.0°C/no base/Nd(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (15/160.0°C/no base/Nd(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (15/160.0°C/no base/Nd(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | ['no base'] |
| La | 1 | (9/160.0°C/no base/La(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (9/160.0°C/no base/La(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Au,Pt | 1 | (45/180.0°C/no base/AuPt/MgO/inert/10.1002/chem.200901501/2009/0) | no data | no data | (45/180.0°C/no base/AuPt/MgO/inert/10.1002/chem.200901501/2009/0) | no data | [] |
| In | 1 | (7/160.0°C/no base/In(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (7/160.0°C/no base/In(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Sc | 1 | (10/160.0°C/no base/Sc(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (10/160.0°C/no base/Sc(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Ce | 1 | (6/160.0°C/no base/Ce(NTf2)s/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (6/160.0°C/no base/Ce(NTf2)s/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Zr | 1 | (7/120.0°C/no base/Zr-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021/0) | (7/120.0°C/no base/Zr-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021/0) | (7/120.0°C/no base/Zr-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021/0) | (7/120.0°C/no base/Zr-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021/0) | (7/120.0°C/no base/Zr-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021/0) | ['no base'] |
| Cs | 1 | (0/160.0°C/no base/Cs(OTf)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (0/160.0°C/no base/Cs(OTf)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| K | 1 | (0/160.0°C/no base/K(NTf2)/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (0/160.0°C/no base/K(NTf2)/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Mg | 1 | (1/160.0°C/no base/Mg(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (1/160.0°C/no base/Mg(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| V | 1 | (0/130.0°C/tBuOK/VCl2/inert/10.1016/j.tet.2011.02.075/2011/0) | no data | no data | no data | no data | [] |
| Ho | 1 | (12/160.0°C/no base/Ho(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (12/160.0°C/no base/Ho(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Gd | 1 | (13/160.0°C/no base/Gd(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (13/160.0°C/no base/Gd(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (13/160.0°C/no base/Gd(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (13/160.0°C/no base/Gd(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (13/160.0°C/no base/Gd(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | ['no base'] |
| Se | 1 | (0/160.0°C/no base/Sr(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (0/160.0°C/no base/Sr(NTf2)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Pr | 1 | (16/160.0°C/no base/Pr(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (16/160.0°C/no base/Pr(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (16/160.0°C/no base/Pr(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (16/160.0°C/no base/Pr(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | (16/160.0°C/no base/Pr(NTf2)3/oxygen/10.1002/ejoc.202000229/2020/microwave) | ['no base'] |
| Ca | 1 | (0/160.0°C/no base/Ca(OTf)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | no data | (0/160.0°C/no base/Ca(OTf)2/oxygen/10.1002/ejoc.202000229/2020/microwave) | no data | [] |
| Cu,Ag | 1 | (560/155.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011/0.1 mol% Cu+ Ag) | (94/155.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011/1 mol% Cu+ Ag) | (94/155.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011/1 mol% Cu+ Ag) | (560/155.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011/0.1 mol% Cu+ Ag) | (94/155.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011/1 mol% Cu+ Ag) | ['no base'] |