Best catalysts by metals for PhNO2 + BnOH process

Data stracture in all cells: (TONmax/T,°C/base/catalyst/atmosphere/doi/comment)

| Metal | Number of papers | Maximal TON among all | Maximal TON among the processes with preparative yields >65% | The lowest temperature among all with preparative yields >65% | The highest TON in the absence of base | The lowest temperature in the absence of base with preparative yields >65% | most popular working bases |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ru | 9 | (97/150.0°C/tBuOK/Ru(II)L1Cl(CO)2 (4)/inert/10.1002/ejic.201100647/L=C6H4(o-PPh2)(o-N=CH)C6H4(O)) | (97/150.0°C/tBuOK/Ru(II)L1Cl(CO)2 (4)/inert/10.1002/ejic.201100647/L=C6H4(o-PPh2)(o-N=CH)C6H4(O)) | (26/100.0°C/KOt-Amyl/(p-cymene)Ru(NHC1^NHC1)ClPF6/inert/10.1002/chem.201603901/0) | (84/150.0°C/no base/Ru(CO)H2(PPh3)3/inert/10.1002/asia.201000945/0) | (27/130.0°C/no base/Ru(CO)H2(PPh3)3/inert/10.1021/ol1020527/0) | ['no base', 'KOt-Amyl', 'K2CO3'] |
| Au | 4 | (1517/150.0°C/K2CO3/Au/Ag-Mo-NR/inert/10.1039/c2cc34178f/0) | (1517/150.0°C/K2CO3/Au/Ag-Mo-NR/inert/10.1039/c2cc34178f/0) | (144/120.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201100393/0) | (228/160.0°C/no base/2.5 wt% Au/NiO/inert/10.1039/c1cc11057h/0) | (144/120.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201100393/0) | ['no base', 'K2CO3'] |
| Ir | 4 | (430/100.0°C/Cs2CO3/Cp*Ir(C^NHC2)I/oxygen/10.1021/acs.organomet.8b00642/0) | (164/100.0°C/Cs2CO3/Cp*Ir(C^NHC2)I/oxygen/10.1021/acs.organomet.8b00642/0) | (81/100.0°C/tBuOK/Cp*IrCl(N^O)1/inert/10.1021/acs.inorgchem.2c00703/0) | no data | no data | ['tBuOK', 'Cs2CO3', 'K2CO3'] |
| Pd | 4 | (960/25.0°C/K3PO4/Pd/NH2-MIL-101(Fe)-2MI(300)/inert/10.1016/j.jcat.2020.05.033/blue LED (0,75W cm-2)) | (960/25.0°C/K3PO4/Pd/NH2-MIL-101(Fe)-2MI(300)/inert/10.1016/j.jcat.2020.05.033/blue LED (0,75W cm-2)) | (227/25.0°C/no base/Pd-Ti-NS/inert/10.1016/j.jcat.2018.02.005/<700nm) | (227/25.0°C/no base/Pd-Ti-NS/inert/10.1016/j.jcat.2018.02.005/<700nm) | (227/25.0°C/no base/Pd-Ti-NS/inert/10.1016/j.jcat.2018.02.005/<700nm) | ['K3PO4', 'tBuOK', 'KOH'] |
| Co | 1 | (6/160.0°C/no base/Co-N-C/CNT@AC/inert/10.1039/C8GC03818J/>420 nm) | (6/160.0°C/no base/Co-N-C/CNT@AC/inert/10.1039/C8GC03818J/>420 nm) | (6/160.0°C/no base/Co-N-C/CNT@AC/inert/10.1039/C8GC03818J/>420 nm) | (6/160.0°C/no base/Co-N-C/CNT@AC/inert/10.1039/C8GC03818J/>420 nm) | (6/160.0°C/no base/Co-N-C/CNT@AC/inert/10.1039/C8GC03818J/>420 nm) | ['no base'] |
| Ni | 1 | (19/20.0°C/no base/Ni/CdS/inert/10.1016/j.jcat.2018.12.011/>420 nm) | no data | no data | (19/20.0°C/no base/Ni/CdS/inert/10.1016/j.jcat.2018.12.011/>420 nm) | no data | [] |
| Mo | 1 | (16/150.0°C/tBuOK/Mo(NHC3)2(CO)4/inert/10.1021/acscatal.1c02956/0) | (16/150.0°C/tBuOK/Mo(NHC3)2(CO)4/inert/10.1021/acscatal.1c02956/0) | (16/150.0°C/tBuOK/Mo(NHC3)2(CO)4/inert/10.1021/acscatal.1c02956/0) | no data | no data | ['tBuOK'] |
| Ag | 1 | (45/140.0°C/Cs2CO3/Ag/Al2O3/inert/10.1039/C5CP00330J/0) | (45/140.0°C/Cs2CO3/Ag/Al2O3/inert/10.1039/C5CP00330J/0) | (41/140.0°C/K2CO3/Ag/Al2O3/inert/10.1039/C5CP00330J/0) | (7/140.0°C/no base/Ag/Al2O3/inert/10.1039/C5CP00330J/0) | no data | ['K2CO3', 'Cs2CO3'] |
| Rh | 1 | (96/100.0°C/Cs2CO3/Cp*Rh(C^NHC2)I/oxygen/10.1021/acs.organomet.8b00642/0) | no data | no data | no data | no data | [] |