Best catalyst for different aliphatic amines

Data stracture in all cells: (TONmax/T,°C/base/catalyst/atmosphere/doi/year/comment)

| Metal | Number of papers | Maximal TON among all | Maximal TON among the processes with preparative yields >65% | The lowest temperature among all with preparative yields >65% | The highest TON in the absence of base | The lowest temperature in the absence of base with preparative yields >65% | most popular working bases |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ru | 47 | (8000/140.0°C/Na/tBu2NNN)Ru(Cl2)(PPh3)/inert/10.1002/ejoc.201901310/2019) | (1040/120.0°C/tBuOK/(NNN1)RuCl2/inert/10.1021/acs.joc.3c00313/2023) | (14/25.0°C/tBuOK/[Ru(p-cymene)Cl2]2/inert/10.1021/jo501273t/2014) | (960/135.0°C/no base/Ru-PNP complex/inert/10.1002/anie.200803229/2008) | (20/100.0°C/no base/CymeneRuCl2/inert/10.1002/ejoc.201300692/2013) | ['no base', 'tBuOK', 'KOH'] |
| Ir | 42 | (2000/130.0°C/no base/Cp*Ir(N^C1)Cl/inert/10.1021/acssuschemeng.3c02803/2023) | (2000/130.0°C/no base/Cp*Ir(N^C1)Cl/inert/10.1021/acssuschemeng.3c02803/2023) | (500/80.0°C/no base/Ir-zeolite/inert/10.1002/cctc.201402101/2014) | (2000/130.0°C/no base/Cp*Ir(N^C1)Cl/inert/10.1021/acssuschemeng.3c02803/2023) | (500/80.0°C/no base/Ir-zeolite/inert/10.1002/cctc.201402101/2014) | ['no base', 'tBuOK', 'NaHCO3'] |
| Pd | 16 | (1300/110.0°C/LiOH/Pd(LA7)/inert/10.1021/acs.inorgchem.1c02515/2022) | (1300/110.0°C/LiOH/Pd(LA7)/inert/10.1021/acs.inorgchem.1c02515/2022) | (33/25.0°C/no base/Pd0,3/TiO2/inert/10.1021/cs300756f/2013) | (442/140.0°C/no base/Pd/Fe2O3/inert/10.1016/j.tetlet.2011.01.059/2011) | (33/25.0°C/no base/Pd0,3/TiO2/inert/10.1021/cs300756f/2013) | ['LiOH', 'no base', 'HCOONa'] |
| Fe | 13 | (44/80.0°C/tBuOK/Fe-PNP-pincer/inert/10.1002/adsc.201600689/2016) | (44/80.0°C/tBuOK/Fe-PNP-pincer/inert/10.1002/adsc.201600689/2016) | (40/80.0°C/tBuOK/Fe-PNP-pincer/inert/10.1002/adsc.201600689/2016) | (35/135.0°C/no base/Cp(O)Fe(CO)3/inert/10.1021/acscatal.5b02160/2015) | (17/110.0°C/no base/Fe(Knokler's cat) with MeCN/inert/10.1002/ejoc.201900209/2019) | ['no base', 'tBuOK'] |
| Pt | 6 | (1940/145.0°C/no base/Pt-Sn/Al2O3/inert/10.1016/j.tet.2016.11.029/2016) | (1940/145.0°C/no base/Pt-Sn/Al2O3/inert/10.1016/j.tet.2016.11.029/2016) | (76/100.0°C/no base/Pt(cod)cl2/inert/10.1002/anie.201106737/2011) | (1940/145.0°C/no base/Pt-Sn/Al2O3/inert/10.1016/j.tet.2016.11.029/2016) | (76/100.0°C/no base/Pt(cod)cl2/inert/10.1002/anie.201106737/2011) | ['no base'] |
| Ni | 5 | (6240/200.0°C/tBuONa/NiNNN/inert/10.1021/acs.organomet.0c00233/2020) | (88/170.0°C/no base/Ni/CaSiO3/inert/10.1016/j.cattod.2013.09.002/2013) | (15/140.0°C/no base/Ni/CaSiO3/inert/10.1016/j.cattod.2013.09.002/2013) | (88/170.0°C/no base/Ni/CaSiO3/inert/10.1016/j.cattod.2013.09.002/2013) | (15/140.0°C/no base/Ni/CaSiO3/inert/10.1016/j.cattod.2013.09.002/2013) | ['no base', 'tBuOK'] |
| Co | 4 | (95/140.0°C/tBuOK/Co@NC-800-L1/inert/10.1039/d1sc05913k/2021) | (95/140.0°C/tBuOK/Co@NC-800-L1/inert/10.1039/d1sc05913k/2021) | (41/110.0°C/no base/Co-PNP-pincer/inert/10.1021/acs.orglett.6b01647/2016) | (46/110.0°C/no base/Co-PNP-pincer/inert/10.1021/acs.orglett.6b01647/2016) | (41/110.0°C/no base/Co-PNP-pincer/inert/10.1021/acs.orglett.6b01647/2016) | ['tBuOK', 'no base'] |
| Mn | 4 | (184/100.0°C/KH/Mn(CO)5Br/inert/10.1021/acs.orglett.9b00832/2019) | (184/100.0°C/KH/Mn(CO)5Br/inert/10.1021/acs.orglett.9b00832/2019) | (184/100.0°C/KH/Mn(CO)5Br/inert/10.1021/acs.orglett.9b00832/2019) | no data | no data | ['KH', 'tBuOK'] |
| no metal | 4 | (890/25.0°C/no base/MFBBCFPc/oxygen/10.1039/d2cy00846g/2022) | (890/25.0°C/no base/MFBBCFPc/oxygen/10.1039/d2cy00846g/2022) | (840/25.0°C/no base/MFBBCFPc/oxygen/10.1039/d2cy00846g/2022) | (890/25.0°C/no base/MFBBCFPc/oxygen/10.1039/d2cy00846g/2022) | (840/25.0°C/no base/MFBBCFPc/oxygen/10.1039/d2cy00846g/2022) | ['no base'] |
| Ag | 3 | (95/100.0°C/KOH/Fe3O4@SiO2-Ag (SMNP-Ag)/oxygen/10.1002/aoc.3720/2017) | (95/100.0°C/KOH/Fe3O4@SiO2-Ag (SMNP-Ag)/oxygen/10.1002/aoc.3720/2017) | (94/100.0°C/KOH/Fe3O4@SiO2-Ag (SMNP-Ag)/oxygen/10.1002/aoc.3720/2017) | no data | no data | ['KOH', 'NaOH'] |
| Cu | 3 | (150/160.0°C/no base/Cu/CeO2-P/inert/10.1016/j.jcat.2023.01.020/2023) | (150/160.0°C/no base/Cu/CeO2-P/inert/10.1016/j.jcat.2023.01.020/2023) | (11/135.0°C/no base/Cu(OH)x/Al2O3/inert/10.1246/cl.2010.1182/2010) | (150/160.0°C/no base/Cu/CeO2-P/inert/10.1016/j.jcat.2023.01.020/2023) | (11/135.0°C/no base/Cu(OH)x/Al2O3/inert/10.1246/cl.2010.1182/2010) | ['no base', 'K2CO3'] |
| Au | 3 | (140/180.0°C/no base/Au/CeO2/inert/10.1002/chem.201201837/2012) | (140/180.0°C/no base/Au/CeO2/inert/10.1002/chem.201201837/2012) | (42/140.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201001848/2010) | (140/180.0°C/no base/Au/CeO2/inert/10.1002/chem.201201837/2012) | (42/140.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201001848/2010) | ['no base'] |
| Rh | 2 | (71/100.0°C/tBuOK/Rh(I)(COD)(NHC)triazoleC6H5/oxygen/10.1021/acs.inorgchem.7b02586/2017) | (71/100.0°C/tBuOK/Rh(I)(COD)(NHC)triazoleC6H5/oxygen/10.1021/acs.inorgchem.7b02586/2017) | (9/80.0°C/no base/Co2Rh2/C/inert/10.1021/acs.joc.8b01109/2018) | (19/120.0°C/no base/Co2Rh2/C/inert/10.1021/acs.joc.8b01109/2018) | (9/80.0°C/no base/Co2Rh2/C/inert/10.1021/acs.joc.8b01109/2018) | ['no base', 'tBuOK'] |
| Os | 2 | (920/200.0°C/no base/OsPincer/inert/10.1039/c1dt10342c/2011) | (920/200.0°C/no base/OsPincer/inert/10.1039/c1dt10342c/2011) | (810/200.0°C/no base/OsPincer/inert/10.1039/c1dt10342c/2011) | (920/200.0°C/no base/OsPincer/inert/10.1039/c1dt10342c/2011) | (810/200.0°C/no base/OsPincer/inert/10.1039/c1dt10342c/2011) | ['no base'] |
| Hf | 1 | (1/140.0°C/no base/Hf-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021) | no data | no data | (1/140.0°C/no base/Hf-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021) | no data | [] |
| Zn | 1 | (21/120.0°C/KOH/CNS@Zn1-AA/inert/10.3390/nano13030445/2023) | no data | no data | no data | no data | [] |
| Ti | 1 | (13/180.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | (13/180.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | (12/180.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | (13/180.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | (12/180.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | ['no base'] |
| Bi | 1 | (90/25.0°C/tBuOK/Bi-S3/S-Vs/inert/10.1039/d2ta06142b/2022) | (90/25.0°C/tBuOK/Bi-S3/S-Vs/inert/10.1039/d2ta06142b/2022) | (90/25.0°C/tBuOK/Bi-S3/S-Vs/inert/10.1039/d2ta06142b/2022) | no data | no data | ['tBuOK'] |
| Cu,Ag | 1 | (96/145.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011) | (96/145.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011) | (96/145.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011) | (96/145.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011) | (96/145.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011) | ['no base'] |