Best catalysts by metals for nitroarene + MeOH process for all catalysts and metals

Data stracture in all cells: (TONmax/T,°C/base/catalyst/atmosphere/doi/comment)

| Metal | Number of papers | Maximal TON among all | Maximal TON among the processes with preparative yields >65% | The lowest temperature among all with preparative yields >65% | The highest TON in the absence of base | The lowest temperature in the absence of base with preparative yields >65% | most popular working bases |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ru | 11 | (184/160.0°C/MeOK/Ru_16/N2/10.1002/cctc.202101630/nan) | (184/160.0°C/MeOK/Ru_16/N2/10.1002/cctc.202101630/nan) | (20/100.0°C/tBuOK/Ru_23/air/10.1039/d3cy00218g/nan) | (25/130.0°C/no base/Ru_23/N2/10.1039/d3cy00218g/nan) | (25/130.0°C/no base/Ru_23/N2/10.1039/d3cy00218g/nan) | ['tBuOK', 'MeONa', 'Cs2CO3'] |
| Ir | 2 | (140/190.0°C/tBuOK/Ir@YSMCNs/Air/10.1002/ajoc.201900140/nan) | (140/190.0°C/tBuOK/Ir@YSMCNs/Air/10.1002/ajoc.201900140/nan) | (114/130.0°C/K2CO3/Cp*Ir(N^N)Cl2/inert/10.1021/acs.joc.1c02625/nan) | no data | no data | ['tBuOK', 'K2CO3'] |
| Pd | 2 | (85/110.0°C/KOH/Pd(OAc)2/inert/10.1002/anie.201814146/nan) | (85/110.0°C/KOH/Pd(OAc)2/inert/10.1002/anie.201814146/nan) | (82/80.0°C/KOH/Pd(OAc)2/inert/10.1002/anie.201814146/nan) | no data | no data | ['KOH', 'K3PO4', 'CsOH'] |
| Pt | 1 | (48/150.0°C/NaOH/5 wt.% Pt/C/oxygen/10.1021/acs.joc.2c02657/nan) | (48/150.0°C/NaOH/5 wt.% Pt/C/oxygen/10.1021/acs.joc.2c02657/nan) | (48/150.0°C/NaOH/5 wt.% Pt/C/oxygen/10.1021/acs.joc.2c02657/nan) | no data | no data | ['NaOH'] |
| Mn | 1 | (48/150.0°C/Cs2CO3/Mn_1/inert/10.1021/acs.orglett.2c03595/nan) | (48/150.0°C/Cs2CO3/Mn_1/inert/10.1021/acs.orglett.2c03595/nan) | (24/140.0°C/Cs2CO3/MnBr(CO)5/Ar/10.1021/acs.orglett.2c03595/nan) | no data | no data | ['Cs2CO3'] |