Best catalyst for different AlkCH2OH and Alk2CHOH

Data stracture in all cells: (TONmax/T,°C/base/catalyst/atmosphere/doi/year/comment)

| Metal | Number of papers | Maximal TON among all | Maximal TON among the processes with preparative yields >65% | The lowest temperature among all with preparative yields >65% | The highest TON in the absence of base | The lowest temperature in the absence of base with preparative yields >65% | most popular working bases |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ru | 7 | (272/150.0°C/no base/Ru(CO)H2(PPh3)3/inert/10.1021/ol1020527/2010) | (272/150.0°C/no base/Ru(CO)H2(PPh3)3/inert/10.1021/ol1020527/2010) | (15/120.0°C/Cs2CO3/cymeneRuCl2/no_data/10.1039/c9qo00544g/2019) | (272/150.0°C/no base/Ru(CO)H2(PPh3)3/inert/10.1021/ol1020527/2010) | (272/150.0°C/no base/Ru(CO)H2(PPh3)3/inert/10.1021/ol1020527/2010) | ['no base', 'K2CO3', 'Na2CO3'] |
| Au | 3 | (1417/150.0°C/K2CO3/Au/Ag-Mo-NR/inert/10.1039/c2cc34178f/2012) | (1417/150.0°C/K2CO3/Au/Ag-Mo-NR/inert/10.1039/c2cc34178f/2012) | (182/120.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201100393/2011) | (182/120.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201100393/2011) | (182/120.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201100393/2011) | ['no base', 'K2CO3'] |
| Pd | 1 | (160/25.0°C/K3PO4/Pd/NH2-MIL-101(Fe)-2MI(300)/inert/10.1016/j.jcat.2020.05.033/2020) | no data | no data | no data | no data | [] |
| Ir | 1 | (108/130.0°C/K2CO3/Cp*Ir(N^N)Cl2/inert/10.1021/acs.joc.1c02625/2021) | (108/130.0°C/K2CO3/Cp*Ir(N^N)Cl2/inert/10.1021/acs.joc.1c02625/2021) | (108/130.0°C/K2CO3/Cp*Ir(N^N)Cl2/inert/10.1021/acs.joc.1c02625/2021) | no data | no data | ['K2CO3'] |
| Mn | 1 | (49/150.0°C/Cs2CO3/Mn_1/inert/10.1021/acs.orglett.2c03595/2022) | (49/150.0°C/Cs2CO3/Mn_1/inert/10.1021/acs.orglett.2c03595/2022) | (49/150.0°C/Cs2CO3/Mn_1/inert/10.1021/acs.orglett.2c03595/2022) | no data | no data | ['Cs2CO3'] |
| Ag | 1 | (0/140.0°C/Cs2CO3/Ag/Al2O3/inert/10.1039/c5cp00330j/2015) | no data | no data | no data | no data | [] |