Best catalyst for different amides

Data stracture in all cells: (TONmax/T,°C/base/catalyst/atmosphere/doi/year/comment)

| Metal | Number of papers | Maximal TON among all | Maximal TON among the processes with preparative yields >65% | The lowest temperature among all with preparative yields >65% | The highest TON in the absence of base | The lowest temperature in the absence of base with preparative yields >65% | most popular working bases |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ru | 10 | (490/130.0°C/tBuOK/Ru_37/no_data/10.1039/d2cy00544a/2022) | (490/130.0°C/tBuOK/Ru_37/no_data/10.1039/d2cy00544a/2022) | (58/85.0°C/KOH/Ru(OH)3/Fe3O4/inert/10.1021/jo200559h/2011) | (19/165.0°C/no base/[Ru(p-cymene)Cl2]2/inert/10.1021/jo102521a/2011) | (19/165.0°C/no base/[Ru(p-cymene)Cl2]2/inert/10.1021/jo102521a/2011) | ['KOH', 'tBuOK', 'K2CO3'] |
| Ir | 6 | (86/100.0°C/K2CO3/Cp*[Ir]NAr ligand/inert/10.1002/chem.201501109/2015) | (86/100.0°C/K2CO3/Cp*[Ir]NAr ligand/inert/10.1002/chem.201501109/2015) | (86/100.0°C/K2CO3/Cp*[Ir]NAr ligand/inert/10.1002/chem.201501109/2015) | (32/110.0°C/no base/IrNHC/inert/10.1002/chem.201201845/2012) | (32/110.0°C/no base/IrNHC/inert/10.1002/chem.201201845/2012) | ['K2CO3', 'Na2CO3', 'KOH'] |
| Pd | 5 | (8800/150.0°C/K2CO3/Pd(Oac)2/oxygen/10.1055/s-0030-1260238/2011) | (8800/150.0°C/K2CO3/Pd(Oac)2/oxygen/10.1055/s-0030-1260238/2011) | (152/100.0°C/K2CO3/Pd(ONO1)PPh3/inert/10.1002/aoc.7228/2023) | (25/140.0°C/no base/Pd(COD)ClSnCl3/oxygen/10.1016/j.tetlet.2016.05.018/2016) | (25/140.0°C/no base/Pd(COD)ClSnCl3/oxygen/10.1016/j.tetlet.2016.05.018/2016) | ['K2CO3', 'Cs2CO3', 'LiOH'] |
| Cu | 4 | (99/135.0°C/K2CO3/Cu(Oac)2/oxygen/10.1039/c1ob06743e/2012) | (99/135.0°C/K2CO3/Cu(Oac)2/oxygen/10.1039/c1ob06743e/2012) | (89/135.0°C/K2CO3/Cu(Oac)2/oxygen/10.1039/c1ob06743e/2012) | (99/150.0°C/no base/Cu(Oac)2/oxygen/10.1002/anie.200901510/2009) | (99/150.0°C/no base/Cu(Oac)2/oxygen/10.1002/anie.200901510/2009) | ['K2CO3', 'tBuOK', 'no base'] |
| Rh | 3 | (198/135.0°C/K2CO3/RhCl(PPh3)3/oxygen/10.1021/jo200862p/2011) | (198/135.0°C/K2CO3/RhCl(PPh3)3/oxygen/10.1021/jo200862p/2011) | (88/110.0°C/KOH/Rh(acac)3/inert/10.1002/adsc.201300061/2013) | no data | no data | ['K2CO3', 'KOH'] |
| no metal | 3 | (88/160.0°C/tBuOK/no/oxygen/10.1016/j.jcat.2022.08.014/2022) | (88/160.0°C/tBuOK/no/oxygen/10.1016/j.jcat.2022.08.014/2022) | (10/90.0°C/no base/PhCH2Br/oxygen/10.1039/c6gc00938g/2016) | (10/130.0°C/no base/PhCH2Br/oxygen/10.1039/c6gc00938g/2016) | (10/90.0°C/no base/PhCH2Br/oxygen/10.1039/c6gc00938g/2016) | ['no base', 'K2CO3', 'NaOH'] |
| Fe | 1 | (20/135.0°C/K2CO3/FeCl2/inert/10.1016/j.tetlet.2010.02.056/2010) | (20/135.0°C/K2CO3/FeCl2/inert/10.1016/j.tetlet.2010.02.056/2010) | (20/135.0°C/K2CO3/FeCl2/inert/10.1016/j.tetlet.2010.02.056/2010) | no data | no data | ['K2CO3'] |
| Mn | 1 | (10/135.0°C/K2CO3/MnO2/oxygen/10.1021/ol202582c/2011) | (10/135.0°C/K2CO3/MnO2/oxygen/10.1021/ol202582c/2011) | (10/135.0°C/K2CO3/MnO2/oxygen/10.1021/ol202582c/2011) | no data | no data | ['K2CO3'] |
| Ag | 1 | (22/160.0°C/K2CO3/Ag-Mo-22 (4.5 mol% Ag, 9 mol% Mo)/inert/10.1002/chem.201001915/2010) | (22/160.0°C/K2CO3/Ag-Mo-22 (4.5 mol% Ag, 9 mol% Mo)/inert/10.1002/chem.201001915/2010) | (19/160.0°C/K2CO3/Ag-Mo-22 (4.5 mol% Ag, 9 mol% Mo)/inert/10.1002/chem.201001915/2010) | no data | no data | ['K2CO3'] |