Best catalysts by metals for amine + MeOH processes for all metals and substrates

Data stracture in all cells: (TONmax/T,°C/base/catalyst/atmosphere/doi/comment)

| Metal | Number of papers | Maximal TON among all | Maximal TON among the processes with preparative yields >65% | The lowest temperature among all with preparative yields >65% | The highest TON in the absence of base | The lowest temperature in the absence of base with preparative yields >65% | most popular working bases |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ru | 15 | (4900/150.0°C/tBuOK/RuH(CO)Cl(bis(2-(diphenylphosphaneyl)ethyl)amine)/Ar/10.1021/acs.orglett.8b01449/nan) | (4900/150.0°C/tBuOK/RuH(CO)Cl(bis(2-(diphenylphosphaneyl)ethyl)amine)/Ar/10.1021/acs.orglett.8b01449/nan) | (48/60.0°C/NaOH/Ru_11/Air/10.1039/d0cy02210a/nan) | (86/180.0°C/no base/RuCl3/oxygen/10.1246/cl.1988.449/nan) | (71/180.0°C/no base/RuCl3/oxygen/10.1246/cl.1988.449/nan) | ['tBuOK', 'MeOK', 'Cs2CO3'] |
| Ir | 4 | (520/150.0°C/Cs2CO3/Ir_1/N2/10.1021/acs.organomet.2c00125/nan) | (368/125.0°C/Cs2CO3/Cp*Ir@CTF/no_data/10.1016/j.jcat.2021.02.030/nan) | (136/115.0°C/Cs2CO3/Cp*Ir@CTF/Air/10.1016/j.jcat.2021.02.030/nan) | no data | no data | ['Cs2CO3', 'tBuOK', 'KOH'] |
| Mn | 2 | (196/140.0°C/Cs2CO3/Mn_1/inert/10.1002/anie.202318763/nan) | (196/140.0°C/Cs2CO3/Mn_1/inert/10.1002/anie.202318763/nan) | (80/120.0°C/K2CO3/Mn_1/inert/10.1002/anie.202318763/nan) | no data | no data | ['Cs2CO3', 'K2CO3'] |
| Co | 1 | (19/160.0°C/tBuOK/Co@NC-800-L1/inert/10.1039/d1sc05913k/nan) | (19/160.0°C/tBuOK/Co@NC-800-L1/inert/10.1039/d1sc05913k/nan) | (19/160.0°C/tBuOK/Co@NC-800-L1/inert/10.1039/d1sc05913k/nan) | no data | no data | ['tBuOK'] |
| Pd | 1 | (25/140.0°C/K2CO3/Pd1Cu0.6–Fe3O4/no_data/10.1039/d2cy00065b/nan) | (25/140.0°C/K2CO3/Pd1Cu0.6–Fe3O4/no_data/10.1039/d2cy00065b/nan) | (19/120.0°C/K2CO3/Pd 1Cu0.6–Fe3O4/no data/10.1039/d2cy00065b/nan) | no data | no data | ['K2CO3', 'KHCO3', 'K3PO4'] |
| Fe | 1 | (20/80.0°C/MeOK/FeCl3/inert/10.1039/d2qo00825d/nan) | no data | no data | no data | no data | [] |
| Re | 1 | (192/140.0°C/Cs2CO3/Re_3/N2/10.1016/j.jcat.2018.08.008/nan) | (192/140.0°C/Cs2CO3/Re_3/N2/10.1016/j.jcat.2018.08.008/nan) | (14/130.0°C/tBuOK/Re_1/N2/10.1016/j.jcat.2018.08.008/nan) | no data | no data | ['Cs2CO3', 'tBuOK', 'K2CO3'] |
| Bi | 1 | (66/25.0°C/tBuOK/Bi-S3/S-Vs/inert/10.1039/d2ta06142b/nan) | (66/25.0°C/tBuOK/Bi-S3/S-Vs/inert/10.1039/d2ta06142b/nan) | (66/25.0°C/tBuOK/Bi-S3/S-Vs/inert/10.1039/d2ta06142b/nan) | no data | no data | ['tBuOK'] |
| Cu | 1 | (8/170.0°C/no base/10Cu-5Co/Al2O3/inert/10.1039/d2gc00827k/nan) | (8/170.0°C/no base/10Cu-5Co/Al2O3/inert/10.1039/d2gc00827k/nan) | (8/170.0°C/no base/10Cu-5Co/Al2O3/inert/10.1039/d2gc00827k/nan) | (8/170.0°C/no base/10Cu-5Co/Al2O3/inert/10.1039/d2gc00827k/nan) | (8/170.0°C/no base/10Cu-5Co/Al2O3/inert/10.1039/d2gc00827k/nan) | ['no base'] |