Best catalyst for different aromatic amines

Data stracture in all cells: (TONmax/T,°C/base/catalyst/atmosphere/doi/year/comment)

| Metal | Number of papers | Maximal TON among all | Maximal TON among the processes with preparative yields >65% | The lowest temperature among all with preparative yields >65% | The highest TON in the absence of base | The lowest temperature in the absence of base with preparative yields >65% | most popular working bases |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ru | 67 | (18500/140.0°C/Na/tBu2NNN)Ru(Cl2)(PPh3)/inert/10.1002/ejoc.201901310/2019) | (7000/100.0°C/tBuOK/[Ru(COD)Cl2]n/inert/10.1016/j.catcom.2017.03.007/2017) | (39/55.0°C/tBuOK/Ru(cod)Cl2/oxygen/10.1002/ejoc.201403636/2015) | (189/180.0°C/no base/RuCl2(PPh3)2/inert/10.1021/jo00192a021/2005) | (89/100.0°C/no base/C6H6-Se-Ru-N-anthracene-Cl/inert/10.1021/acs.organomet.8b00908/2019) | ['tBuOK', 'KOH', 'no base'] |
| Ir | 62 | (3960/70.0°C/tBuOK/IrPNP pincer/inert/10.1002/chem.201402952/2014) | (3960/70.0°C/tBuOK/IrPNP pincer/inert/10.1002/chem.201402952/2014) | (186/25.0°C/tBuOK/IrNHC/inert/10.1039/c3cc42669f/2013) | (500/80.0°C/no base/Ir-zeolite/inert/10.1002/cctc.201402101/2014) | (58/40.0°C/no base/Ir_2/inert/10.1002/ejoc.202301105/2024) | ['no base', 'tBuOK', 'K2CO3'] |
| Pd | 23 | (4619/120.0°C/LiOH/Pd-SiO2XantPhosOAc/inert/10.1039/c5ra07225e/2015) | (4619/120.0°C/LiOH/Pd-SiO2XantPhosOAc/inert/10.1039/c5ra07225e/2015) | (32/25.0°C/no base/Pd0,3/TiO2/inert/10.1021/cs300756f/2013) | (720/25.0°C/no base/PdCl2/CdS/inert/10.1021/acscatal.2c00433/2022) | (32/25.0°C/no base/Pd0,3/TiO2/inert/10.1021/cs300756f/2013) | ['no base', 'LiOH', 'CsOH'] |
| Fe | 18 | (330/135.0°C/KOH/Fe20-SA@NSC/inert/10.1039/d1ta07673f/2021) | (330/135.0°C/KOH/Fe20-SA@NSC/inert/10.1039/d1ta07673f/2021) | (51/25.0°C/no base/Fe/TiO2/inert/10.1016/j.apcatb.2022.121264/2022) | (58/25.0°C/no base/Fe/TiO2/inert/10.1016/j.apcatb.2022.121264/2022) | (51/25.0°C/no base/Fe/TiO2/inert/10.1016/j.apcatb.2022.121264/2022) | ['no base', 'tBuOK', 'KOH'] |
| Co | 17 | (669/140.0°C/tBuOK/Co1−N3P1/inert/10.1021/jacs.4c07197/2024) | (669/140.0°C/tBuOK/Co1−N3P1/inert/10.1021/jacs.4c07197/2024) | (45/80.0°C/tBuOK/Co-PNP-pincer/inert/10.1002/anie.201507955/2015) | (48/110.0°C/no base/Co-PNP-pincer/inert/10.1021/acs.orglett.6b01647/2016) | (47/110.0°C/no base/Co-PNP-pincer/inert/10.1021/acs.orglett.6b01647/2016) | ['tBuOK', 'no base', 'KOH'] |
| Ni | 14 | (24960/200.0°C/tBuONa/NiNNN/inert/10.1021/acs.organomet.0c00233/2020) | (920/130.0°C/tBuOK/NiN4Br/inert/10.1039/d2gc02206k/2022) | (92/110.0°C/tBuOK/NiBr2(PPh3)2/oxygen/10.1021/acs.joc.1c00510/2021) | (99/144.0°C/no base/Ni/θ-Al2O3/inert/10.1021/cs4001267/2013) | (31/120.0°C/no base/Ni/Ru@SBA/inert/10.1021/acssuschemeng.2c01092/2022) | ['tBuOK', 'KOH', 'no base'] |
| Cu | 13 | (363/100.0°C/KOH/Cu/Magnetitt/oxygen/10.1039/c3gc40818c/2013) | (363/100.0°C/KOH/Cu/Magnetitt/oxygen/10.1039/c3gc40818c/2013) | (73/25.0°C/no base/[CuNNO(OAc)]2/oxygen/10.1039/d2dt01771g/2022) | (196/160.0°C/no base/Cu/CeO2-P/inert/10.1016/j.jcat.2023.01.020/2023) | (77/25.0°C/no base/[CuNNO(OAc)]2/oxygen/10.1039/d2dt01771g/2022) | ['no base', 'tBuOK', 'KOH'] |
| no metal | 13 | (1700/25.0°C/no base/MFBBCFPc/oxygen/10.1039/d2cy00846g/2022) | (1700/25.0°C/no base/MFBBCFPc/oxygen/10.1039/d2cy00846g/2022) | (1660/25.0°C/no base/MFBBCFPc/oxygen/10.1039/d2cy00846g/2022) | (1700/25.0°C/no base/MFBBCFPc/oxygen/10.1039/d2cy00846g/2022) | (810/25.0°C/no base/MFBBCFPc/oxygen/10.1039/d2cy00846g/2022) | ['tBuOK', 'no base', 'KOH'] |
| Mn | 11 | (198/60.0°C/KH/Mn(CO)5Br/inert/10.1021/acs.orglett.9b00832/2019) | (198/100.0°C/tBuOK/Mn_2/inert/10.1002/cctc.202500113/2025) | (55/25.0°C/tBuOK/Mn(CO)3(NHC)2/inert/10.1039/c9cc02989c/2019) | no data | no data | ['tBuOK', 'KH', 'CsOH'] |
| Ag | 6 | (106/110.0°C/NaOH/Ag@MnO2/oxygen/10.1177/1747519821989963/2021) | (106/110.0°C/NaOH/Ag@MnO2/oxygen/10.1177/1747519821989963/2021) | (95/100.0°C/KOH/Fe3O4@SiO2-Ag (SMNP-Ag)/oxygen/10.1002/aoc.3720/2017) | (24/145.0°C/no base/Ag/Al2P3-5/inert/10.1002/cctc.200900209/2009) | (24/145.0°C/no base/Ag/Al2P3-5/inert/10.1002/cctc.200900209/2009) | ['tBuOK', 'NaOH', 'KOH'] |
| Rh | 6 | (97/100.0°C/tBuOK/Rh(I)(COD)(NHC)triazoleC6H5/oxygen/10.1021/acs.inorgchem.7b02586/2017) | (97/100.0°C/tBuOK/Rh(I)(COD)(NHC)triazoleC6H5/oxygen/10.1021/acs.inorgchem.7b02586/2017) | (96/100.0°C/tBuOK/Rh(I)(COD)(NHC)triazoleC6H5/oxygen/10.1021/acs.inorgchem.7b02586/2017) | (90/100.0°C/no base/Cp*-S-Rh-N-anthracene-Cl/inert/10.1021/acs.organomet.8b00908/2019) | (90/100.0°C/no base/Cp*-S-Rh-N-anthracene-Cl/inert/10.1021/acs.organomet.8b00908/2019) | ['no base', 'tBuOK', 'KOH'] |
| Au | 5 | (196/120.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201001848/2010) | (196/120.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201001848/2010) | (9/100.0°C/tBuOK/Ph3PAuCl/inert/10.1016/j.tet.2014.10.007/2014) | (196/120.0°C/no base/Au/TiO2-VS/inert/10.1002/chem.201001848/2010) | (20/110.0°C/no base/Au/ZrO2/inert/10.1016/j.apcata.2011.11.017/2011) | ['no base', 'tBuOK'] |
| Pt | 5 | (1960/145.0°C/no base/Pt-Sn/Al2O3/inert/10.1016/j.tet.2016.11.029/2016) | (1960/145.0°C/no base/Pt-Sn/Al2O3/inert/10.1016/j.tet.2016.11.029/2016) | (94/130.0°C/tBuOK/Pt/C/no_data/10.1021/acs.joc.2c02657/2023) | (1960/145.0°C/no base/Pt-Sn/Al2O3/inert/10.1016/j.tet.2016.11.029/2016) | (1900/145.0°C/no base/Pt-Sn/Al2O3/inert/10.1016/j.tet.2016.11.029/2016) | ['no base', 'tBuOK'] |
| Zn | 3 | (106/120.0°C/KOH/CNS@Zn1-AA/inert/10.3390/nano13030445/2023) | (106/120.0°C/KOH/CNS@Zn1-AA/inert/10.3390/nano13030445/2023) | (23/120.0°C/tBuOK/(NNN2)ZnCl2/inert/10.1021/acs.joc.2c01773/2022) | no data | no data | ['tBuOK', 'KOH'] |
| Ti | 3 | (19/180.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | (19/180.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | (13/100.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | (19/180.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | (13/100.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | ['KOH', 'no base'] |
| Os | 2 | (670/200.0°C/no base/OsPincer/inert/10.1039/c1dt10342c/2011) | (670/200.0°C/no base/OsPincer/inert/10.1039/c1dt10342c/2011) | (670/200.0°C/no base/OsPincer/inert/10.1039/c1dt10342c/2011) | (670/200.0°C/no base/OsPincer/inert/10.1039/c1dt10342c/2011) | (670/200.0°C/no base/OsPincer/inert/10.1039/c1dt10342c/2011) | ['no base'] |
| W | 2 | (98/130.0°C/tBuOK/w(co)6/inert/10.1002/cssc.202002830/2020) | (98/130.0°C/tBuOK/w(co)6/inert/10.1002/cssc.202002830/2020) | (94/130.0°C/tBuOK/w(co)6/inert/10.1002/cssc.202002830/2020) | (13/140.0°C/no base/10WO3/ZrO2/oxygen/10.1039/d2ra00198e/2022) | no data | ['tBuOK'] |
| Mo | 2 | (46/130.0°C/tBuOK/MoNHC/inert/10.1021/acscatal.1c02956/2021) | (46/130.0°C/tBuOK/MoNHC/inert/10.1021/acscatal.1c02956/2021) | (24/120.0°C/tBuOK/Mo(CO)6/oxygen/10.1016/j.mcat.2021.111415/2021) | no data | no data | ['tBuOK'] |
| Re | 1 | (10/150.0°C/no base/ReH7(Pcy3)2/inert/10.1016/j.tetlet.2014.05.068/2014) | (10/150.0°C/no base/ReH7(Pcy3)2/inert/10.1016/j.tetlet.2014.05.068/2014) | (8/150.0°C/no base/ReH7(Pcy3)2/inert/10.1016/j.tetlet.2014.05.068/2014) | (10/150.0°C/no base/ReH7(Pcy3)2/inert/10.1016/j.tetlet.2014.05.068/2014) | (8/150.0°C/no base/ReH7(Pcy3)2/inert/10.1016/j.tetlet.2014.05.068/2014) | ['no base'] |
| Bi | 1 | (100/25.0°C/tBuOK/Bi-S3/S-Vs/inert/10.1039/d2ta06142b/2022) | (100/25.0°C/tBuOK/Bi-S3/S-Vs/inert/10.1039/d2ta06142b/2022) | (94/25.0°C/tBuOK/Bi-S3/S-Vs/inert/10.1039/d2ta06142b/2022) | no data | no data | ['tBuOK'] |
| Hf | 1 | (8/120.0°C/no base/Hf-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021) | (8/120.0°C/no base/Hf-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021) | (7/120.0°C/no base/Hf-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021) | (8/120.0°C/no base/Hf-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021) | (7/120.0°C/no base/Hf-MOF-808_H2O/oxygen/10.1021/acssuschemeng.1c04903/2021) | ['no base'] |
| Sm | 1 | (28/140.0°C/tBuOK/SmI2/inert/10.1021/acs.joc.9b00717/2019) | (28/140.0°C/tBuOK/SmI2/inert/10.1021/acs.joc.9b00717/2019) | (27/140.0°C/tBuOK/SmI2/inert/10.1021/acs.joc.9b00717/2019) | no data | no data | ['tBuOK'] |
| Cr | 1 | (33/150.0°C/tBuOK/CrNNN/inert/10.1002/anie.202001704/2020) | (33/150.0°C/tBuOK/CrNNN/inert/10.1002/anie.202001704/2020) | (28/150.0°C/tBuOK/CrNNN/inert/10.1002/anie.202001704/2020) | no data | no data | ['tBuOK'] |
| Cu,Ag | 1 | (92/155.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011) | (92/155.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011) | (80/145.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011) | (92/155.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011) | (80/145.0°C/no base/Cu0.95Ag0.05/Al2O3/inert/10.1039/c1ra00560j/2011) | ['no base'] |