Best catalyst for different heteroaromatic amines before 2022

Data stracture in all cells: (TONmax/T,°C/base/catalyst/atmosphere/doi/year/comment)

| Metal | Number of papers | Maximal TON among all | Maximal TON among the processes with preparative yields >65% | The lowest temperature among all with preparative yields >65% | The highest TON in the absence of base | The lowest temperature in the absence of base with preparative yields >65% | most popular working bases |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ru | 28 | (9500/100.0°C/tBuOK/[Ru(COD)Cl2]n/inert/10.1016/j.catcom.2017.03.007/2017) | (9500/100.0°C/tBuOK/[Ru(COD)Cl2]n/inert/10.1016/j.catcom.2017.03.007/2017) | (332/70.0°C/tBuOK/RuPNHC/inert/10.1039/d1ob00362c/2021) | (37/110.0°C/no base/[Ru(p-cymene)Cl2]2/inert/10.1021/ja807323a/2009) | (37/110.0°C/no base/[Ru(p-cymene)Cl2]2/inert/10.1021/ja807323a/2009) | ['tBuOK', 'KOH', 'no base'] |
| Ir | 25 | (930/70.0°C/tBuOK/[IrCl(cod)]2/inert/10.1002/chem.200802318/2009) | (930/70.0°C/tBuOK/[IrCl(cod)]2/inert/10.1002/chem.200802318/2009) | (92/50.0°C/tBuOK/IrNHC/inert/10.1039/c3cc42669f/2013) | (95/110.0°C/no base/GIrNC/oxygen/10.1039/d1ra09052f/2022) | (59/110.0°C/no base/IrNHC/inert/10.1002/chem.201201845/2012) | ['tBuOK', 'NaOH', 'K2CO3'] |
| Pd | 14 | (1820/110.0°C/LiOH/Pd(LA7)/inert/10.1021/acs.inorgchem.1c02515/2022) | (1820/110.0°C/LiOH/Pd(LA7)/inert/10.1021/acs.inorgchem.1c02515/2022) | (84/100.0°C/LiOH/Pd2((AcO)pirazoleAr3)2/inert/10.1016/j.tet.2017.03.001/2017) | (465/120.0°C/no base/Fe10Pd1NC50/inert/10.1039/d0gc03725g/2020) | (455/120.0°C/no base/Fe10Pd1NC50/inert/10.1039/d0gc03725g/2020) | ['no base', 'CsOH', 'LiOH'] |
| Fe | 10 | (307/135.0°C/KOH/Fe20-SA@NSC/inert/10.1039/d1ta07673f/2021) | (307/135.0°C/KOH/Fe20-SA@NSC/inert/10.1039/d1ta07673f/2021) | (37/80.0°C/tBuOK/Fe-PNP-pincer/inert/10.1002/adsc.201600689/2016) | (28/160.0°C/no base/FeBr3 / prolinone/inert/10.1002/anie.201006660/2011) | (13/110.0°C/no base/Fe(Knokler's cat) with MeCN/inert/10.1002/ejoc.201900209/2019) | ['tBuOK', 'tBuONa', 'KOH'] |
| Ni | 7 | (32640/200.0°C/tBuONa/NiNNN/inert/10.1021/acs.organomet.0c00233/2020) | (32640/200.0°C/tBuONa/NiNNN/inert/10.1021/acs.organomet.0c00233/2020) | (95/110.0°C/tBuOK/NiBr2(PPh3)2/oxygen/10.1021/acs.joc.1c00510/2021) | no data | no data | ['tBuOK', 'KOH', 'KOt-Amyl'] |
| Co | 6 | (100/140.0°C/tBuOK/Co@NC-800-L1/inert/10.1039/d1sc05913k/2021) | (100/140.0°C/tBuOK/Co@NC-800-L1/inert/10.1039/d1sc05913k/2021) | (44/80.0°C/tBuOK/Co-PNP-pincer/inert/10.1002/anie.201507955/2015) | no data | no data | ['tBuOK', 'KOH'] |
| no metal | 6 | (72/90.0°C/tBuOK/no/oxygen/10.1016/j.jcat.2022.08.014/2022) | (72/90.0°C/tBuOK/no/oxygen/10.1016/j.jcat.2022.08.014/2022) | (72/90.0°C/tBuOK/no/oxygen/10.1016/j.jcat.2022.08.014/2022) | no data | no data | ['tBuOK', 'NaOH'] |
| Mn | 4 | (31/80.0°C/tBuOK/Mn-PNP-pincer/inert/10.1038/ncomms12641/2016) | (31/80.0°C/tBuOK/Mn-PNP-pincer/inert/10.1038/ncomms12641/2016) | (28/80.0°C/tBuOK/Mn-PNP-pincer/inert/10.1038/ncomms12641/2016) | no data | no data | ['tBuOK', 'CsOH', 'NaOH'] |
| Cu | 4 | (228/120.0°C/KOH/Copper(I) complex/oxygen/10.1016/j.poly.2014.12.015/2015) | (228/120.0°C/KOH/Copper(I) complex/oxygen/10.1016/j.poly.2014.12.015/2015) | (220/120.0°C/KOH/Copper(I) complex/oxygen/10.1016/j.poly.2014.12.015/2015) | no data | no data | ['NaOH', 'tBuOK', 'KOH'] |
| Rh | 3 | (160/150.0°C/K2CO3/RhCl(PPh3)3/oxygen/10.1021/jo200862p/2011) | (160/150.0°C/K2CO3/RhCl(PPh3)3/oxygen/10.1021/jo200862p/2011) | (97/100.0°C/tBuOK/Rh(I)(COD)(NHC)triazoleC6H5/oxygen/10.1021/acs.inorgchem.7b02586/2017) | no data | no data | ['K2CO3', 'tBuOK', 'NaOH'] |
| Zn | 2 | (31/120.0°C/tBuOK/(NNN2)ZnCl2/inert/10.1021/acs.joc.2c01773/2022) | (31/120.0°C/tBuOK/(NNN2)ZnCl2/inert/10.1021/acs.joc.2c01773/2022) | (26/120.0°C/tBuOK/(NNN2)ZnCl2/inert/10.1021/acs.joc.2c01773/2022) | no data | no data | ['tBuOK'] |
| W | 1 | (93/130.0°C/tBuOK/w(co)6/inert/10.1002/cssc.202002830/2020) | (93/130.0°C/tBuOK/w(co)6/inert/10.1002/cssc.202002830/2020) | (86/130.0°C/tBuOK/w(co)6/inert/10.1002/cssc.202002830/2020) | no data | no data | ['tBuOK'] |
| Pt | 1 | (396/145.0°C/no base/PtSn/Al2O3 1:3/inert/10.1002/chem.201101725/2011) | (396/145.0°C/no base/PtSn/Al2O3 1:3/inert/10.1002/chem.201101725/2011) | (184/145.0°C/no base/PtSn/Al2O3 1:3/inert/10.1002/chem.201101725/2011) | (396/145.0°C/no base/PtSn/Al2O3 1:3/inert/10.1002/chem.201101725/2011) | (184/145.0°C/no base/PtSn/Al2O3 1:3/inert/10.1002/chem.201101725/2011) | ['no base'] |
| Sm | 1 | (26/140.0°C/tBuOK/SmI2/inert/10.1021/acs.joc.9b00717/2019) | (26/140.0°C/tBuOK/SmI2/inert/10.1021/acs.joc.9b00717/2019) | (26/140.0°C/tBuOK/SmI2/inert/10.1021/acs.joc.9b00717/2019) | no data | no data | ['tBuOK'] |
| Cr | 1 | (29/150.0°C/tBuOK/CrNNN/inert/10.1002/anie.202001704/2020) | (29/150.0°C/tBuOK/CrNNN/inert/10.1002/anie.202001704/2020) | (29/150.0°C/tBuOK/CrNNN/inert/10.1002/anie.202001704/2020) | no data | no data | ['tBuOK'] |
| Ti | 1 | (11/160.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | (11/160.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | (11/160.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | (11/160.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | (11/160.0°C/no base/Ti(NTf2)4/oxygen/10.1002/ejoc.202000413/2020) | ['no base'] |
| Au | 1 | (9/100.0°C/tBuOK/Ph3PAuCl/inert/10.1016/j.tet.2014.10.007/2014) | (9/100.0°C/tBuOK/Ph3PAuCl/inert/10.1016/j.tet.2014.10.007/2014) | (9/100.0°C/tBuOK/Ph3PAuCl/inert/10.1016/j.tet.2014.10.007/2014) | no data | no data | ['tBuOK'] |
| Ag | 1 | (92/110.0°C/NaOH/Ag@MnO2/oxygen/10.1177/1747519821989963/2021) | (92/110.0°C/NaOH/Ag@MnO2/oxygen/10.1177/1747519821989963/2021) | (92/110.0°C/NaOH/Ag@MnO2/oxygen/10.1177/1747519821989963/2021) | no data | no data | ['NaOH'] |